Nonlocal transport in a 2D semimetal, a topological insulator
and a Dirac fermions system based on HgTe quantum wells
Z.D. Kvon
Institute of Semiconductor Physics, Novosibirsk, Russia
1. Local and nonlocal transport. Nonlocal transport in the QHE regime.
2. Energy spectrum of HgTe quantum wells: insulator → DF → 2DTI → 2DS
3. Nonlocal transport in a 2D semimetal in the QHE regime.
4. Nonlocal transport in a 2D TI.
5. Giant nonlocality in 2D Dirac fermions system.

---
Co-authors:
- G.M.Gusev
- (Universidade de S˜ao Paulo, Brazil)
- O.A.Shegai
- D.A.Kozlov
- E.B.Olshanetsky
- N.N. Mikhailov
- S.A. Dvoretsky
Measurements
MBE growth

---
Local and nonlocal transport
In a Drude conductor the nonlocal response is exponentialy weak:
;	RnL 26,35 ≈
RL14,23 = ρxx (L/W)

---
Edge current state picture of the QHE
Rxx = 0
Rxy = h/3e2
n-HgTe 21 nm QW
i =1
Rxx ~ h/e2
h/3e2<Rxy <h/2e2
i =2
i =3
Rxx = 0
Rxy = h/2e2
So in the QHE regime one has a dissipationless transport when the Fermi level lies between the Landau
levels and a dissipative transport when the Fermi level goes through a Landau level center.

---
Nonlocal transport in the QHE regime
In the QHE regime one has the local dissipative resistance RL ~ h/e2 and the non-local resistance RnL = αRL
α = (10-2 - 10-1 ) depending on the conductor parameters and the contact configuration. Nevertheless the nonlocal signal is much larger than in the Drude case due to the edge current state contribution.

---
Semiconductors with direct and inverted band structure
EV ; p (l=1)
CdTe
HgTe
EC ; s (l=0)
J=1/2;
j=±1/2
J=3/2;
j=±3/2;
j=±1/2
J=1/2;
j=±1/2;
Direct band structure
J=l+s;
g≈1.5eV
EC ; p (l=1)
J=3/2;j = ±1/2
EV ; p (l=1)
J=3/2;j = ±3/2
EV ; s (l=0)
J=1/2
EV ; p (l=1)
J=1/2
Inverted band structure
g  - 0.35 eV

---
Energy spectrum in a HgTe quantum well: a 2D semimetal, a 2D topological insulator and a 2D Dirac fermions
(M.I.Dyakonov and A.V.Khaetskii, JETP, 55, 917 (1982), Y.Lin-Liu, L.Sham, PRB, 32, 5561 (1985); L.G.Gerchikov and A.V.Subashiev, PSS(b), 160, 443(1990), B.Bernevig et al, Science, 314, 1757 (2006), E.G.Novik et al. PRB, 83, 193304(2011))
dw, nm

---
2D semimetal in (100) HgTe quantum well

---
Energy spectrum
The band overlap Δ and, correspondingly,
The semimetal state is due to the strain in quantum well which is the result of the HgTe and CdTe lattice mismatch. The overlap magnitude depends on the QW surface orientation. In particular,
Δ(013) ≈ 5 meV, а Δ(100) ≈ 1 meV

---
QHE in 2D semimetal in the intermediate magnetic fields
Percolation network in a 2D
e-h system in magnetic field in the
vicinity of the CNP

---
QHE in a 2D semimetal in intermediate magnetic field:
local and nonlocal transport
In the intermediate magnetic fields (B < 4 T) the conventional nonlocal QHE transport is
observed on the electron side and only very weakly at the CNP and the hole side of R(Vg).

---
QHE in a 2D semimetal. High resistance local and non-local transport at the CNP in strong magnetic fields

---
Dissipative local and nonlocal transport in the vicinity of CNP
Local and nonlocal resistances in (Vg , B) coordinates. T = 1.6 K.

---
Local and nonlocal transport in the vicinity of CNP. Temperature dependence.
Dashed traces were calculated by means of edge plus bulk transport model developed in Abanin et al, PRL, 98, 196806 (2007) and V.T.Dogopolov et al, Sol.St.Comm, 78, 999 (1991).
In particular, the large peak in the local and nonlocal resistance is mostly due to the edge transport at the CNP. The suppression of the peaks away from the CNP is due to a short circuiting of the edge
transport by the bulk conductivity.

---
Interpretation: dissipative transport of counterpropagating electron and hole edge currents (EC) with backscattering
(Abanin et al, PRL, Phys. Rev. Lett. 98, 196806)
electron EC
hole EC
h-like LL
gap
e-like LL
bulk insulator
Realization of such Landau levels position
at B > 4 T is supported by
Oleg Raichev’s recent calculations

---
Diffusive local and nonlocal transport in a 2D TI (QSHE)
Edge current states and their conductance in a 2D TI (QSHE)
The upper 1D single-mode wire
In a ballistic case
G = Gu + Gl = I/(μleft – μright) =
e2/h + e2/h = 2e2/h
insulator
L
In a diffusive case (max{lu, ll} << L)
G = Gu + Gl = [(lu + ll)/L]e2/h =
The lower 1D single-mode wire

---
2D TI conductance: multi-probes measurements
There is no difference between local and nonlocal resistance in a 2D TI in ballistic and diffusive cases because in either case we have 1D wires along the sample edges. And if in the case of ballistic transport we need to use Landauer-Buttiker formalism to calculate the resistance, in the diffusive case it is enough to know the Kirhgoph law from a school physics cousse.

---
Diffusive local and nonlocal transport in a 2D TI
on the basis (013) HgTe QW
Few microns samples
Macroscopic samples
0.5 mm
For all samples and measurement configurations a conductance G = (0.25 – 0.03)e2/h

---
In-plain magnetic field induced transition
2D TI – 2D metal: expirement
Macroscopic samples
Few microns samples

---
In-plain magnetic field induced transition
2D TI – 2D metal: theory (O.Raichev, PRB, 85, 045310 (2012))
The 2D electron spectrum for Bc looks like a Dirac cone with a parabolic branch attached [Fig. 6(a)] and resembles the spectrum of bulk CdxHg1−xTexalloy at x = 0.16. When the magnetic field exceeds Bc, there exist two parabolic (near k = 0) branches with effective masses of opposite signs;these branches are degenerate at k = 0 [Fig. 6(b)]. The band picture, therefore, is similar to that of bulk HgTe, with the difference that the order of energy bands is inverted and the bands are not spin degenerate. The 2D gapless state described here seems to be a unique example of this kind in the physics of 2D electron systems. It is interesting to notice that the high-energy branch of the edge states does not disappear when the system becomes gapless.

---
Linear positive magnetoresistance caused by the breaking of the TRS in a normal magnetic field
According to the theory (J. Maciejko, X-L. Qi, and S-C. Zhang, Phys. Rev. B 82, 155310 (2010) :
Δσ(B)/σ = - α|B|;
α strongly depends on disorder strength W
Our experiments are in agreement with the case of a small disorder W < Eg

---
Edge current state in a 2DTI as single-mode long disorder wire
Theoretical picture
(Mirlin, Gornyi and Polyakov, PRB, 75, 085421 (2007)
2D TI single-mode 12 μm disorderd wire
Experiment with V-grooves single-mode wires
E.Levy et al, PRB, 85, 045315 (2012)
So in a 2D TI single-mode wire a very weak temperature
dependence is observed contrary to the theory and
experiments on AlGaAs/GaAs.
T(K)

---
Dissipative edge current transport: QHE, QHE in graphene and 2D semimetal in the vicinity of the CNP, a 2D TI at zero magnetic field
Electron systems realized in a 2D semimetal in the QHE regime at the CNP and in a 2D TI at zero magnetic field are topologically similar. In both cases we have a gap in the bulk and two counter-propagating edge current states on the quantum well edges. In a 2D semimetal these are one hole and one electron edge state. In a 2D TI these are two electron edge states with opposite spin directions. These states can be considered as long single mode diffusive wires. So their further study seems interesting as related to Luttinger liquid physics.
P-band or h-like LL
EF
S band or e-like LL

---
Late nonlocality news: giant nonlocality in the Dirac point
How to get Dirac fermions in HgTe QW?
Gerchikov and Subashiev (Fiz . Tekh. Poluprov. 23, 2187 (1989), Phys.Stat.Sol., 160, 443 (1990) )

---
More accurate calculations
E.G.Novik (unpublished): influence of strain
O.E. Raichev, Phys.Rev. B85, 045310 (2012)

---
Transport response at B=0 for 6.6 nm QW: two ranges
Vg> -1V:
Dirac fermions
Vg< -1V: DF and
heavy holes
Fig.2. ρxx (Vg) at different temperatures

---
Giant nonlocality at the Dirac point

---
Hall effect origin
So we come to a preliminary conclusion that this giant nonlocality is similar to that observed recently in
graphene at low temperatures (T < 20 K) (Abanin et al, Science, 332, 328(2011)) and described as a Zeeman induced spin Hall effect. But unlike to graphene it is anomaously large (ξ > 1 at B = 1 T, ξ = σnH/σxx ) and extends on the macroscopic scale (hundreds of microns).
Further study is necessary.

---
No back-scattering !
Spin is uniquely connected with momentum due to time resersal symmetry (TRS)
  |1>	|2>
<1|2> = 0 if spin dependent interaction is absent
s
p
p
s